Cable Jelly (Filling / Flooding Compound)

| Sr. # | Characteristics | Filling Compound | Flooding Compound |
| --- | --- | --- | --- |
|  |  | Paragel THXO | Para-Gel |  |
| 1. | Colour | - | Doesn't Obscure | - |
| 2. | Specific Gravity @ 27oC | - | 0.91 +/- 0.02 | - |
| 3. | Drop Point oC Min. | 120 - 150 (to specific requirements) | 85 - 105 (to specific requirements) | 85 - 110 (to specific requirements) |
| 4. | Cone Penetration @ 25oC, mm, Min. | 200 - 400 (to specific requirements) | 35 - 60 (to specific requirements) | 80 - 200 (to specific requirements) |
| 5. | Flash Point, oC, Min. | 230 | >232 | 200 |
| 6. | Volume Resistance @ 100oC, ohm- CM, Min. | 0.8 | 1 x 1010 | - |
| 7. | Neutralisation Number, mg KOH/g Max. | - | 0.05 | - |
| 8. | Viscosity @ 100oC, cSt, Min. | - | 85 - 105 | - |
| 9. | Stability Test @ 70oC, for 5 days | Shall Pass | No Separation of Constituents of compound | No Separation of Constituents of compound |
| 10. | Power Factor @ 23oC, 1 Mhz., Max. | - | 0.0005 | - |
| 11. | Permitivity @ 20oC, 1 Mhz., Max | - | 2.3 | - |
| 12. | Absorption % Max. | - | 8.0 | - |
| 13. | Acidity mg of KOH | - | Neutral | - |

For further information please send us an Email on sales@paraffinoil.com