Light Liquid Paraffin Oil

| Characteristics | Liquid Liquid Paraffin Oil |
| --- | --- |
| Appearance | Colourless and clear oily liquid free from odour |
| Solubility | Insoluble in water and alcohol |
| Weight / ml @ 20oC | Between 44 to 56 |
| U.V. Absorption of 1 cm | 0.83 to 0.88 |
| Kinematic Viscosity@ 40oC | 10 to 30 |
| Colour Saybolt | +30 |
| Reaction | Neutral |
| Flash Point COC oC | 170 to 210 |
| Packing | Net 175 kgs MS Drums |
| Applications | Cosmetics, Hair Oils, Baby Oils etc. |

For further information please send us an Email on sales@paraffinoil.com