White Petroleum Jelly

| Characteristics | Petroleum Jelly Snow White (IP/BP/USP) |
| --- | --- |
| Description | Snow White translucent solid mass, odourless, tasteless |
| Solubility | Insoluble in water and alcohol |
| Melting Range oC | Between 48 to 58 |
| U.V. Absorption of 1 cm Layer of 0.05% w/v Soln. in ISO-octane at 290 mm | Extinction, E= 0.04 to 0.1 (Limit Max. 0.5) |
| Acidity or Alkalinity | Passes |
| Sulphated Ash | 0.05 % (Limit max. 0.1%) |
| Consistency at 25oC | Between 175 to 200 (Limit 100 to 300) |
| Additional Tests |  |
| Specific Gravity @ 60oC | 0.81 to 0.83 |
| Volatile Matter | 0.6 to 0.8 % |
| Organic Acid | Passes the test |
| Bleeding Number | Maximum 28 mm (Limit max. 30 mm) |
| Carbonisable Impurities | - |
| Uses | Skin ointments, Ophthalmic ointments, Dermal Ointments, Balms, Cold Creams etc. covering Cosmetics and Pharmaceuticals |
| Packing | Net 170 kgs / 15 kgs in Drums (MS or HDPE PRICE DIFFERS FOR BOTH) and Tins |

For further information please send us an Email on sales@paraffinoil.com

The information provided on this page is, to the best of our knowledge accurate, however, it is subject to change without prior notice.  We assume no liability for the completeness of it or errors in it.  Current and final specifications and datasheets can be obtained by contacting us on sales@paraffinoils.com