Lubricants & Engineering Products’ Specifications

| Cylinder Oil |  |
| --- | --- |
| Characteristics | Specifications |
| Appearance | clear bright |
| Color | Dark Brown |
| Odour | -- |
| Sp. Gravity at 30 deg. C | 0.94 |
| Flash Point (PMCC) deg.C (min) | 260 |
| Kinetic Viscosity @ 40 deg. C | 1400-1700 cSt |
| Kinetic Viscosity @ 100 deg. C | 62.5 |
| V.I. | 83.3 |

| Karoil - 80DA |  |
| --- | --- |
| Characteristics | Specifications |
| Appearance | clear and bright |
| Color | Water White |
| Flash Point (PMCC) deg.C (min) | 84 |
| Kinetic Viscosity @ 40 deg. C | 2.05 |
| Sp. Gravity at 29.5 deg. C | 0.777 |
| Odour | Not Offensive |
| Pour point deg. C | < - 20 |
| TAN mg KOH/gm | 0.02 |
| Copper Corrosion | Passes |
| Aromatic Content, w/w(%) | 3.2 |
| Distillation deg. C (IBP) | 205 |
| Distillation deg. C (FBP) | 280 |

| Karfree-60 |  |
| --- | --- |
| Characteristics | Karfree-60 |
| Appearance | Clear and Bright |
| Color | Water White |
| Flash Point (PMCC) deg.C (min) | 140 min. |
| Kinetic Viscosity @ 40 deg. C | 8.5±1.0 |
| Sp. Gravity at 29.5 deg. C | 0.8 |
| Odour | Odourless |
| Pour point deg. C | -28 |
| Copper Corrosion | Passes |
| Aromatic Content, w/w(%) | < 1.0 |
| TAN mg KOH/gm | 0.003 max |
| V.I.Min | 106 |

| Karoil - 61 |  |
| --- | --- |
| Characteristics | Specifications |
| Appearance | Clear and Bright |
| Color | Water White |
| Flash Point (PMCC) deg.C (min) | 78 |
| Kinetic Viscosity @ 40 deg. C | 1.6 |
| Sp. Gravity at 29.5 deg. C | 0.8 |
| Odour | Not Offensive |
| Aniline point deg. C | 61 |
| Boiling range deg. C (IBP) | 198 |
| Boiling Range deg. C (FBP) | 242 |
| Carbon Type Cp(%) | 62 |
| Carbon Type Ca(%) | 20 |
| Carbon Type Cn(%) | 18 |

| Karoil - 74 |  |
| --- | --- |
| Characteristics | Specifications |
| Appearance | Clear and Bright |
| Color | Water white |
| Flash Point (PMCC) deg.C (min) | 76 |
| Kinetic Viscosity @ 40 deg. C | 1.58 |
| Sp. Gravity at 29.5 deg. C | 0.785 |
| Odour | Not offensive |
| Aniline point deg. C | 74 |
| Aromatic w/w% | 3.00 |
| Boiling range deg. C (IBP) | 190 |
| Boiling Range deg. C (FBP) | 235 |
| Dry Point Deg.C | 235 |

| Refrigeration Oils |  |  |  |
| --- | --- | --- | --- |
| Characteristics | Specifications |  |  |
|  | VG-32 | VG-46 | VG-68 |
| Appearance | Clear and Bright | Clear and Bright | Clear and Bright |
| Color | 1.0 | 1.0 | 1.0 |
| Odour | Not Offensive | Not Offensive | Not Offensive |
| Sp. Gravity at 29.5 deg. C | 0.861 | 0.861 | 0.861 |
| Flash Point (PMCC) Deg.C (min) | 154 | 160 | 186 |
| Kinetic Viscosity @ 40 deg. C | 32 ± 2 cSt | 46 ± 3 cSt | 64.0 cSt |
| @37.8 Deg. C | -- | -- | -- |
| Pour point deg. C | -34 | -34 | -34 |
| Aniline point deg. C | -- | -- | -- |

| Characteristics | Specifications |  |
| --- | --- | --- |
|  | Aluminium Rolling Oil | Looms Oil |
| Appearance | Clear and Bright | Clear and Bright |
| Color | < 0.5 | Dark Brown |
| Odour | Not Offensive | Not Offensive |
| Sp. Gravity at 29.5 deg. C | 0.815 | 0.945 |
| Flash Point (PMCC) deg.C (min) | 110 | 190 |
| Kinetic Viscosity @ 40 deg. C | 2.7 | -- |
| Viscosity at 30 deg.C(FB4) | -- | 150sec |
| Aromatic Content,wt% | 12.0 | -- |
| Aniline point deg. C | 70 | N.A. |
| Distillation deg. C (IBP) | 240 | -- |
| Distillation deg. C (FBP) | 281 | -- |

For further information please send us an Email on sales@paraffinoil.com